## Slide 1: Novel Additives to Improve the Environmental Footprint of Fabric Laundering
SYFA Spring Conference 2023

## Slide 2: Overview
v
  The Laundry Dilemma
  Goulston’s Background
  Goulston Tackling the Dilemma
  Wrap-Up

## Slide 3: Overview
v
  The Laundry Dilemma
  Goulston’s Background
  Goulston Tackling the Dilemma
  Wrap-Up

## Slide 4: Today’s Laundry Dilemma
Clothes must be washed, but at what cost?
Source: FreePik
Notes: https://www.freepik.com/free-photos-vectors/dirty-clothes

## Slide 5: Today’s Laundry Dilemma
Garment Laundering
Energy Consumption
Microplastics into
Water Systems
Energy Consumption
  675-877 kWh used on average, for home dryer by Americans annually
Microplastics
  Estimated 878 tonnes of plastic microfibers released by U.S. and Canadian home laundering annually
Sources: Arcadia, 2017, The Folde, n.d., Ellam, 2019
Notes: Energy Consumption:
300 loads x 2.25 kWh = 675 kWh; 390 loads x 2.25 kWh = 877.5 kWh
300-390 loads of laundry per year for Americans (P&G)
2.25 kWh per launder

## Slide 6: Today’s Laundry Dilemma
47%
Cooling & Heating
Water Heater
14%
13%
12%
4%
4%
3%
2%
1%
Computer
Dishwasher
TV & Accessories
Electric Oven
Refrigerator
Lighting
Clothes Washing & Drying
Clothes Washing & Drying
71% from Drying
Sources: Taylor & Francis, 2010 and Desjardins, 2016

## Slide 7: Today’s Laundry Dilemma
24%
7%
3.7%
2%
0.3%
35%
28%
Source: IUCN, 2017
Marine Coatings
Road Markings
City Dust
Personal Care Products
Plastic Pellets
Synthetic Textiles - Laundering
Vehicle Tires
Contribution of Microplastics to Oceans
Notes: AATCC:
-Fiber fragment is <5 mm
-Microfiber has diameter <1 micron

## Slide 8: Approach to Laundry Dilemma
Reduced
Energy
Consumption
Reduced
Microplastics into
Water Systems
®
additives

## Slide 9: Overview
v
  The Laundry Dilemma
  Goulston’s Background
  Goulston Tackling the Dilemma
  Wrap-Up

## Slide 10: Goulston’s History
George A. Goulston Company established in Scituate, MA
Monroe, NC facility opened
Acquired by Takemoto Oil & Fat Co., LTD
Opened first ester manufacturing facility in Monroe, NC
Opened North Plant facility in Monroe, NC
1937
1969
1988
2014
2023

## Slide 11: Headquarters in Monroe, NC
Centralized R&D and production on
23-acre manufacturing site
Over 300,000 ft2 with over 70 mixing vessels and eight reactors
North Plant commissioned in Q1 2023, providing expanded reaction capabilities
Notes: 8 reactors, both hot oil and steam, ranging from 800 to 8,000 gallons (3-30 kiloliters)
Expanded synthesis capabilities for esters, amides, phosphates, quaternary compounds, imidazolines, betaines, and condensation polymers
North Plant provides vertical integration for Goulston while also allowing us to more efficiently develop new chemistries with scale from lab to pilot to production scale

## Slide 12: Expertise in Surface Modification
Core Areas
  Spandex
  Carpet
  Textile filament
  Industrial filament
  Staple fibers & nonwovens
  Polymer additives
  Plastic films
  Antimicrobials
  Laundry aids
Emerging Technologies
  Specialty polymers
  Conductive fibers and additives
  Cosmetic additives

## Slide 13: Expertise in Surface Modification
In-depth understanding of surface interactions
What is a surface?
  Interaction between two phases
    Solid-liquid
    Liquid-gas
    Solid-gas

## Slide 14: Expertise in Surface Modification
In-depth understanding of surface interactions
What is a surface?
  Interaction between two phases
    Solid-liquid
    Liquid-gas
    Solid-gas
Surface modifications change the way surfaces behave

## Slide 15: Expertise in Surface Modification
A fiber finish is a coating which provides specific properties to the fiber surface that:
  Improves the fiber manufacturing process
  Improves downstream performance
  Provides desired end-use properties
  Provides added value to the fiber, fabric, and/or garment
Source: Ecotextile

## Slide 16: Overview
v
  The Laundry Dilemma
  Goulston’s Background
  Goulston Tackling the Dilemma
  Wrap-Up

## Slide 17: DryFast® Additives
Anchors to Filaments
Protects Filaments
Manages Moisture Transport

## Slide 18: DryFast® Additives

## Slide 19: DryFast® Additives
Manages Moisture Transport
Reduces dry time
Reduces energy consumption

## Slide 20: DryFast® Additives

## Slide 21: DryFast® Additives
Protects Filaments
Reduces shedding
Reduces microfiber release in water systems
Notes: AATCC:
-Fiber fragment is <5 mm
-Microfiber has diameter <1 micron

## Slide 22: DryFast® Additives
Chemistry Application
Final Stage
(Ex. Dyeing / Finishing)
Post Treatment
(Ex. Laundering)
In-Process
(Ex. Coning Oil Step)

## Slide 23: Moisture Management Approach
Manages Moisture Transport
Notes: When washing garments, particularly activewear, with standard home laundry detergent (Tide), wicking properties are lost. Incorporating DryFast® with detergent (on its own or added to the detergent formulation) will preserve the garment’s wicking performance provided when worn off-the-shelf or restore wicking performance once its lost. DryFast® functions by moving moisture outward to form a thin wet layer, taking less energy to allow the moisture to evaporate and the garment to dry.
Most activewear and synthetic garment suppliers recommend not using fabric softeners on the garments as traditional fabric softeners are hydrophobic, bead up on the surface, and inhibit wicking. This also causes clothes to take longer to dry. DryFast® is safe to soften on all synthetics to protect wearability while protecting wicking performance.

## Slide 24: Moisture Management Approach
Manages Moisture Transport
  DryFast® provides enhanced wicking
  DryFast® replenishes wicking length lost through laundering
Chart: Wetted Radius of DryFast® Treated Fabric
| Top Maximum Wetted Radius (mm) | Bottom Maximum Wetted Radius (mm)
Unwashed Control | 20 | 21.67
10 Washes - No Additive | 18.33 | 21.67
10 Washes - DryFast® | 20 | 23.33
Notes: AATCC Test Method 195 for MMT
ASTM D1776 for conditioning (27 +/-2C, 65 +/- 5% RH)
Top layer fabric = next to skin

## Slide 25: Moisture Management Approach
Manages Moisture Transport
  DryFast® restores and enhances one-way transport
  DryFast® provides enhanced overall moisture management capacity
Chart: MMT of DryFast® Treated Fabric
| Unwashed Control | 10 Washes - No Additive | 10 Washes - DryFast®
Accumulative One-Way Transport Index | 146.817 | 137.877 | 148.684
OMMC | 0.46 | 0.461 | 0.512
Notes: AATCC Test Method 195 for MMT
ASTM D1776 for conditioning (27 +/-2C, 65 +/- 5% RH)
Top layer fabric = next to skin

## Slide 26: Moisture Management Approach
Manages Moisture Transport
-10%
-33%
-8%
-33%
  8-33% reductions in dry time using DryFast® additives in home dryer
  Performance improved with synthetics
Notes: Samples:
100% Terry cloth towels
52/48 Polyester/Cotton sheets
100% Cotton sheets
100% Polyester wipes

## Slide 27: Moisture Management Approach
-37%
Manages Moisture Transport
0
0
20
40
60
80
100
20
40
60
80
100
Time in Dryer (min)
Untreated Control
1% DryFast®
  37% reduction in dry time using DryFast® additives
  At 55 minutes,
    Untreated 82% dry
    DryFast® 100% dry
  80% polyester, 20% cotton shirts used
Mass Loss of Water (%)
100% Dry
82% Dry
Notes: Completed on 80/20 blend of Polyester/Cotton

## Slide 28: Moisture Management Approach
  DryFast® significantly enhances vertical wicking
  DryFast® imparts wash durability
Manages Moisture Transport
Chart: Durability of DryFast® Treated Fiber
| 0 | 1 | 5 | 10 | 15 | 30
DryFast® 0 Washes | 0 | 6 | 11 | 14 | 16 | 19
DryFast® 10 Washes | 0 | 5.5 | 10 | 13 | 15 | 18
Untreated 10 Washes | 0 | 3 | 5 | 7 | 8 | 10
®
®

## Slide 29: Microfiber Reduction Approach
AATCC TM212-2021
Fiber Fragment Release During Home Laundering
Washing Option B – No detergent
Drying Option B – Oven dried filters
Socks used – 98% PET / 2% Spandex
Protects Filaments

## Slide 30: Microfiber Reduction Approach
Protects Filaments
Vacuum

## Slide 31: Microfiber Reduction Approach
Untreated Control
additive
®
Protects Filaments

## Slide 32: Microfiber Reduction Approach
Chart: Impact on Fiber Fragmentation
| DryFast® Additive 1.0% FOY | DryFast® Additive 0.5% FOY | Untreated Control
 | 0.89 | 0.81739 | 0
Protects Filaments
®
®
89%
82%

## Slide 33: Microfiber Reduction Approach
Chart: Impact on Fiber Fragmentation
Protects Filaments
Untreated Control
DryFast® Additive – 1% FOY
X150
X150
Clear differentiation in fiber counts
Differentiation in fiber fragment sizes difficult to discern

## Slide 34: Microfiber Reduction Approach
Protects Filaments
Size (d. nm)
Size Distribution by Number
15
10
5
0.1
0
1
10
100
1000
10000
Untreated Control
DryFast® Additive – 1% FOY
x = 80.75 ± 25.76
_
x = 182.7 ± 60.28
_
20
25
Number (%)

## Slide 35: Overview
v
  The Laundry Dilemma
  Goulston’s Background
  Goulston Tackling the Dilemma
  Wrap-Up

## Slide 36: Future of DryFast® Additives
  DryFast ® additives pass OECD 302B in 21 days
  Achieved >80% sustainability of DryFast® products through bio-based and circular feedstocks
  Continued innovation to approach complete sustainability
Sustainability
Notes: COD = ~2,000,000 mg O2 /L

## Slide 37: Summary
Reduced
Energy
Consumption
Reduced
Microplastics into
Water Systems
®
additives
Based on 300 average loads (675 kWh), 54-222 kWh can be saved annually
Based on 878 average tonnes, up to 781 tonnes can be prevented annually

## Slide 38: Final Thought
We are stronger together than we are alone
- Walter Payton
Source: National Science Foundation

## Slide 39: Matt Bridges R&D Manager – Filament mbridges@goulston.com
Darren Mond Senior Research Associate dmond@goulston.com
Thank you!

## Slide 40: References
Boucher, J., & Friot, D. (2017). International Union for Conservation of Nature. Primary Microplastics in the Oceans: A Global Evaluation of Sources. Retrieved April 2023, from https://portals.iucn.org/library/sites/library/files/documents/2017-002-En.pdf
Desjardins, J. (2016, November 14). What uses the most energy in your home? Visual Capitalist. Retrieved April 2023, from https://www.visualcapitalist.com/what-uses-the-most-energy-home/
Electricity costs for 10 key household products. Arcadia. (2017, July 17). Retrieved April 2023, from https://blog.arcadia.com/electricity-costs-10-key-household-products/
Ellam, S. (2022, August 23). Laundry releases trillions of plastic microfibers into the Ocean. Ocean Wise. Retrieved April 2023, from https://www.ocean.org/blog/canadian-and-us-laundry-releases-trillions-of-plastic-microfibers-into-the-ocean/
Golden, J. S., Subramanian, V., Irizarri, G. M. A. U., White, P., & Meier, F. (2010, March 5). Energy and carbon impact from residential laundry in the United States. Taylor & Francis. Retrieved April 2023, from https://www.tandfonline.com/doi/full/10.1080/19438150903541873
Wait?!? how much time do people spend on laundry? The Folde. (n.d.). Retrieved April 2023, from https://www.thefolde.com/how-much-time-do-people-spend-on-laundry/#:~:text=Simple%20math%20shows%20that%20people,600%20per%20year%20on%20detergent.
Dirty-clothes. (2023). Freepik. Retrieved April 2023, from https://www.freepik.com/free-photos-vectors/dirty-clothes.
Fabric with water droplets. (2020). Ecotextile News. Retrieved April 2023, from https://www.ecotextile.com/2020033025889/dyes-chemicals-news/eu-likely-to-ban-c6-based-textile-coatings.html.
Weave_h. (2015). National Science Foundation. Retrieved April 2023, from https://www.nsf.gov/news/mmg/mmg_disp.jsp?med_id=76146.
Visual References